## Slide 1: Materials In Vacuum Technology
مواد در فناوری خلأ

## Slide 3: Vapor Pressure (Vaporization and Condensation)

## Slide 5: Outgassing in Vacuum

## Slide 6
Outgassing
خروج گازهای جذب شده در جداره های داخلی سیستم به داخل سیستم خلأ، که به صورت آرام صورت می گیرد اصطلاحا آوتگسینگ گفته می شود و با افزایش دما افزایش مییابد .
نمایش داده میشود و واحد آن فشار-حجم بر زمان است.K و با
مهمترین گازی که در ابتدا دفع میشود بخار آب است که عمدتا از راه هوا جذب سطوح داخلی میشود.سایر گازها به مقادیر کمتر نظیر هیدروژن، مونو و دی اکسید کربن و.....عمدتا در زمان فرایند های آماده سازی سطوح اتفاق می افتد.
6

## Slide 7: تبدیلات (PV )

## Slide 8: Materials Outgassing
ماده | x(Torr-lit)/(sec- پس از 1 ساعت | x(Torr-lit)/(sec- پس از 4 ساعت
فولاد زنگ زده | 44 | 5.5
فولاد زنگ نزن | 1.75 | 0.4
فولاد زنگ نزن براق و چربی زدایی شده | 1 | 0.05
آلومینیم شسته شده | 1 | 
مس | 23 | 
برنج | 10 | 2.5
نایلون | 120 | 60
لاستیک سیلیکون گاززدایی شده با نیتروژن | 13 | 
اورینگ نیتریل | 10 | 6
اورینگ نیتریل پخته شده در 100 درجه 4 ساعت | 10 | 0.7
اورینگ وایتون | 10 | 3
اورینگ نیتریل پخته شده در 150درجه 4 ساعت | 0.1 | 0.003
ماده |  | 
فولاد زنگ زده | 44 | 5.5
فولاد زنگ نزن | 1.75 | 0.4
فولاد زنگ نزن براق و چربی زدایی شده | 1 | 0.05
آلومینیم شسته شده | 1 | 
مس | 23 | 
برنج | 10 | 2.5
نایلون | 120 | 60
لاستیک سیلیکون گاززدایی شده با نیتروژن | 13 | 
اورینگ نیتریل | 10 | 6
اورینگ نیتریل پخته شده در 100 درجه 4 ساعت | 10 | 0.7
اورینگ وایتون | 10 | 3
اورینگ نیتریل پخته شده در 150درجه 4 ساعت | 0.1 | 0.003

## Slide 10: Materials in Vacuum
Outgassing of materials can be the limiting factor in achieving good vacuum.
  It is usually best to use all stainless steel, aluminum, glass and copper.
  Elastomer gaskets and o-rings should be specifically manufactured for vacuum applications.
NEVER USE:
  Brass, zinc, or other alloys without first looking up the outgassing rate (should be less than 10-4 W/m2).
*O’Hanlon, Users Guide to Vacuum Technology, Wiley (1980).

## Slide 11
STAINLESS STEEL
  Most common choice in HV and UHV systems
  304 – common,
  304L – Low carbon variant of 304 especially in UHV systems
  321 – for when low magnetic permeability is required
BUT…. Avoid 303 grade – contains sulphur and tends to outgas
COPPER (Oxygen-free) C10100 & C10200
  ‘Oxygen-free’ type is widely used
  Easy to machine
  Impermeable to hydrogen and helium
  Low sensitivity to water vapour
TUNGSTEN
  Can be used at high temperatures
  Can be used for filaments
BUT…Becomes brittle when work-hardened
ALUMINIUM & AL ALLOYS
  Low outgassing
  Easy to machine
  Low weight and lower cost
BUT…Some alloys contain a high proportion of Zinc ; Must NOT be anodised; Poor strength at high temperatures ;
Not easy to weld
Materials to use: Metals

## Slide 12
PORCELAIN AND ALUMINA
  Excellent electrical insulation
  Non-porous if fully vitrified
  Low coefficient of thermal expansion – usable to 1500oC
BOROSILICATE GLASS
  Used for viewports
  Can be machined and joined with metals
  Low coefficient of thermal expansion – resistant to thermal shock
Materials to use: Polymers
PTFE-TEFLON
  Good electrical insulator
  Tolerant to high temperatures
  Low outgassing
BUT…Cannot be used as a barrier between vacuum and atmosphere as it is permeable to gases
KAPTON
  Good electrical insulator
  Tolerant to high temperatures
  Very low outgassing
  Available in tape and film form
PEEK – Polyether ether ketone
  Excellent mechanical & chemical resistance
  Suitable for UHV applications
  Very low outgassing
BUT…Has a melting point of 343oC
VITON
  Used for demountable seals (‘O’ rings etc.)
  Can also be used as a seating face in valves
  Good electrical insulator
  Good chemical resistance
  Bakeable to 200oC
Materials to use: Ceramics

## Slide 13
CADMIUM
Often present in the form of plating (fasteners etc.) or in some brazing alloys
ZINC
Is a problem in high vacuum and high temperatures. Present in some alloys like brass (some electrical fittings)
MAGNESIUM
  Low melting point (650oC at atmosphere). Contains free hydrogen gas
PVC
  Often found in wire insulation, dust caps etc.
POLYMERS
  Many have an affinity to water
  Especially plastic tapes. Mould release residue can be an issue too. Polymers may generate a static charge attracting dust
  Nylon has a high outgassing rate
Materials To Avoid
because of the high vapor pressure

## Slide 14: Permeability and Other Gas Sources
A single viton seal on a flange, gate valve bonnet or pump inlet will limit the ultimate pressure to >10-9 mbar.
Unbaked systems will rarely reach better than 10-8 mbar.
Trapped volumes or virtual leaks will increase pump down time.
Microscopic air leaks can limit the ultimate pressure.
The use of a mass spectrometer on a regular basis will help to identify the nature of the gas source.